Spectrum Label: Spectrum 1

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 70202

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.66 | 917157 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | 0.00 | 0.00 | 0.00 | Na2O |  |
| Mg K | 4.13 | 3.61 | 6.85 | MgO |  |
| Al K | 35.63 | 28.03 | 67.32 | Al2O3 |  |
| Si K | 7.41 | 5.60 | 15.84 | SiO2 |  |
| P K | -0.02 | -0.02 | -0.05 | P2O5 |  |
| S K | 0.01 | 0.01 | 0.03 | SO3 |  |
| Cl K | -0.08 | -0.05 | 0.00 |  |  |
| K K | -0.07 | -0.04 | -0.09 | K2O |  |
| Ca K | 0.13 | 0.07 | 0.19 | CaO |  |
| Fe L | 7.71 | 2.93 | 9.92 | FeO |  |
| Ni L | 0.06 | 0.02 | 0.08 | NiO |  |
| O | 45.10 | 59.84 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Spectrum Label: Spectrum 2

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 69031

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.78 | 918548 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | 0.10 | 0.09 | 0.13 | Na2O |  |
| Mg K | 3.84 | 3.37 | 6.37 | MgO |  |
| Al K | 36.23 | 28.63 | 68.46 | Al2O3 |  |
| Si K | 6.54 | 4.96 | 13.98 | SiO2 |  |
| P K | 0.01 | 0.01 | 0.02 | P2O5 |  |
| S K | 0.08 | 0.05 | 0.19 | SO3 |  |
| Cl K | 0.02 | 0.01 | 0.00 |  |  |
| K K | 0.12 | 0.07 | 0.14 | K2O |  |
| Ca K | -0.14 | -0.07 | -0.19 | CaO |  |
| Fe L | 8.80 | 3.36 | 11.33 | FeO |  |
| Ni L | -0.36 | -0.13 | -0.45 | NiO |  |
| O | 44.76 | 59.65 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Spectrum Label: Spectrum 3

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 70210

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.72 | 917337 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | 0.08 | 0.07 | 0.11 | Na2O |  |
| Mg K | 3.81 | 3.33 | 6.32 | MgO |  |
| Al K | 37.66 | 29.63 | 71.15 | Al2O3 |  |
| Si K | 5.74 | 4.34 | 12.29 | SiO2 |  |
| P K | 0.12 | 0.08 | 0.28 | P2O5 |  |
| S K | 0.02 | 0.01 | 0.04 | SO3 |  |
| Cl K | -0.04 | -0.02 | 0.00 |  |  |
| K K | -0.12 | -0.07 | -0.15 | K2O |  |
| Ca K | -0.01 | -0.01 | -0.02 | CaO |  |
| Fe L | 7.76 | 2.95 | 9.98 | FeO |  |
| Ni L | 0.02 | 0.01 | 0.03 | NiO |  |
| O | 44.96 | 59.66 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Spectrum Label: Spectrum 4

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 68351

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.71 | 917742 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | -0.12 | -0.12 | -0.16 | Na2O |  |
| Mg K | 1.63 | 1.49 | 2.71 | MgO |  |
| Al K | 32.37 | 26.53 | 61.16 | Al2O3 |  |
| Si K | 2.37 | 1.86 | 5.06 | SiO2 |  |
| P K | -0.16 | -0.11 | -0.36 | P2O5 |  |
| S K | 5.08 | 3.51 | 12.69 | SO3 |  |
| Cl K | 0.11 | 0.07 | 0.00 |  |  |
| K K | 0.02 | 0.01 | 0.02 | K2O |  |
| Ca K | -0.04 | -0.02 | -0.05 | CaO |  |
| Fe L | 14.98 | 5.93 | 19.27 | FeO |  |
| Ni L | -0.35 | -0.13 | -0.45 | NiO |  |
| O | 44.11 | 60.98 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Spectrum Label: Spectrum 5

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 69579

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.70 | 917083 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | 0.06 | 0.06 | 0.08 | Na2O |  |
| Mg K | 5.16 | 4.60 | 8.55 | MgO |  |
| Al K | 34.12 | 27.41 | 64.48 | Al2O3 |  |
| Si K | 5.48 | 4.23 | 11.72 | SiO2 |  |
| P K | 0.24 | 0.16 | 0.54 | P2O5 |  |
| S K | 0.09 | 0.06 | 0.22 | SO3 |  |
| Cl K | -0.04 | -0.03 | 0.00 |  |  |
| K K | -0.29 | -0.16 | -0.34 | K2O |  |
| Ca K | 0.08 | 0.04 | 0.11 | CaO |  |
| Fe L | 12.16 | 4.72 | 15.64 | FeO |  |
| Ni L | -0.75 | -0.28 | -0.95 | NiO |  |
| O | 43.70 | 59.19 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Spectrum Label: Spectrum 6

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 69354

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.72 | 915956 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | 0.09 | 0.08 | 0.12 | Na2O |  |
| Mg K | 3.90 | 3.39 | 6.47 | MgO |  |
| Al K | 36.59 | 28.62 | 69.13 | Al2O3 |  |
| Si K | 7.16 | 5.38 | 15.32 | SiO2 |  |
| P K | 0.16 | 0.11 | 0.37 | P2O5 |  |
| S K | -0.02 | -0.01 | -0.04 | SO3 |  |
| Cl K | -0.05 | -0.03 | 0.00 |  |  |
| K K | -0.23 | -0.12 | -0.27 | K2O |  |
| Ca K | 0.09 | 0.05 | 0.13 | CaO |  |
| Fe L | 6.74 | 2.55 | 8.67 | FeO |  |
| Ni L | 0.12 | 0.04 | 0.15 | NiO |  |
| O | 45.44 | 59.94 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Spectrum Label: Spectrum 7

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 68809

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.65 | 918350 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | 0.03 | 0.03 | 0.04 | Na2O |  |
| Mg K | 1.24 | 1.13 | 2.05 | MgO |  |
| Al K | 32.76 | 26.95 | 61.91 | Al2O3 |  |
| Si K | 2.38 | 1.88 | 5.10 | SiO2 |  |
| P K | -0.27 | -0.20 | -0.63 | P2O5 |  |
| S K | 4.80 | 3.32 | 11.98 | SO3 |  |
| Cl K | -0.03 | -0.02 | 0.00 |  |  |
| K K | 0.02 | 0.01 | 0.03 | K2O |  |
| Ca K | 0.02 | 0.01 | 0.03 | CaO |  |
| Fe L | 15.09 | 6.00 | 19.41 | FeO |  |
| Ni L | 0.09 | 0.03 | 0.11 | NiO |  |
| O | 43.87 | 60.85 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Spectrum Label: Spectrum 8

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 68128

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.70 | 917226 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | 0.34 | 0.31 | 0.46 | Na2O |  |
| Mg K | 2.95 | 2.56 | 4.89 | MgO |  |
| Al K | 37.70 | 29.47 | 71.24 | Al2O3 |  |
| Si K | 6.80 | 5.11 | 14.56 | SiO2 |  |
| P K | 0.04 | 0.03 | 0.10 | P2O5 |  |
| S K | 0.05 | 0.03 | 0.11 | SO3 |  |
| Cl K | 0.13 | 0.08 | 0.00 |  |  |
| K K | 0.07 | 0.04 | 0.09 | K2O |  |
| Ca K | 0.43 | 0.23 | 0.61 | CaO |  |
| Fe L | 5.98 | 2.26 | 7.70 | FeO |  |
| Ni L | 0.10 | 0.03 | 0.12 | NiO |  |
| O | 45.40 | 59.85 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Spectrum Label: Spectrum 9

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 66390

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.67 | 918812 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | -0.26 | -0.23 | -0.35 | Na2O |  |
| Mg K | 3.02 | 2.56 | 5.01 | MgO |  |
| Al K | 41.91 | 32.01 | 79.19 | Al2O3 |  |
| Si K | 6.29 | 4.62 | 13.46 | SiO2 |  |
| P K | 0.03 | 0.02 | 0.08 | P2O5 |  |
| S K | -0.18 | -0.12 | -0.46 | SO3 |  |
| Cl K | 0.12 | 0.07 | 0.00 |  |  |
| K K | -0.21 | -0.11 | -0.25 | K2O |  |
| Ca K | 0.04 | 0.02 | 0.05 | CaO |  |
| Fe L | 2.46 | 0.91 | 3.17 | FeO |  |
| Ni L | -0.01 | -0.01 | -0.02 | NiO |  |
| O | 46.78 | 60.26 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Spectrum Label: Spectrum 10

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 69433

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.59 | 917257 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | 1.50 | 1.34 | 2.02 | Na2O |  |
| Mg K | 1.63 | 1.38 | 2.71 | MgO |  |
| Al K | 38.27 | 29.26 | 72.31 | Al2O3 |  |
| Si K | 8.60 | 6.31 | 18.39 | SiO2 |  |
| P K | 0.20 | 0.14 | 0.47 | P2O5 |  |
| S K | 0.13 | 0.09 | 0.34 | SO3 |  |
| Cl K | -0.05 | -0.03 | 0.00 |  |  |
| K K | 0.14 | 0.08 | 0.17 | K2O |  |
| Ca K | 0.54 | 0.28 | 0.76 | CaO |  |
| Fe L | 2.36 | 0.87 | 3.04 | FeO |  |
| Ni L | -0.11 | -0.04 | -0.14 | NiO |  |
| O | 46.78 | 60.32 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Spectrum Label: Spectrum 11

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 68063

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.66 | 917644 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | 0.16 | 0.15 | 0.22 | Na2O |  |
| Mg K | 2.47 | 2.15 | 4.09 | MgO |  |
| Al K | 36.37 | 28.57 | 68.72 | Al2O3 |  |
| Si K | 5.22 | 3.94 | 11.17 | SiO2 |  |
| P K | 0.03 | 0.02 | 0.06 | P2O5 |  |
| S K | 2.43 | 1.60 | 6.06 | SO3 |  |
| Cl K | -0.10 | -0.06 | 0.00 |  |  |
| K K | 0.02 | 0.01 | 0.02 | K2O |  |
| Ca K | 0.10 | 0.05 | 0.13 | CaO |  |
| Fe L | 7.55 | 2.87 | 9.71 | FeO |  |
| Ni L | -0.06 | -0.02 | -0.08 | NiO |  |
| O | 45.83 | 60.72 |  |  |  |
| Totals | 100.00 |  |  |  |  |

Spectrum Label: Spectrum 12

Livetime 90.0 s

Acquisition geometry ( degrees ):

Tilt = 0.0

Azimuth = 0.0

Elevation = 30.0

Accelerating voltage = 10.00 kV

Total spectrum counts = 69192

| Sample data : | Energy (eV) | Resn. (eV) | Area |
| --- | --- | --- | --- |
| Strobe : | 3.8 | 52.70 | 918044 |
| Optimization data : Manganese K series |  |  |  |
|  | Energy (eV) | Resn. (eV) | Area |
| Strobe : | .1 | 53.38 | 1150729 |
| Optimization element : | 5892.6 | 129.89 | 573533 |

Spectrum processing :

No peaks omitted

Processing option : Oxygen by stoichiometry (Normalised)

Number of iterations = 1

Standard :

Na    Albite   1-Jun-1999 12:00 AM

Mg    MgO   1-Jun-1999 12:00 AM

Al    Al2O3   1-Jun-1999 12:00 AM

Si    SiO2   1-Jun-1999 12:00 AM

P    GaP   1-Jun-1999 12:00 AM

S    FeS2   1-Jun-1999 12:00 AM

Cl    KCl   1-Jun-1999 12:00 AM

K    MAD-10 Feldspar   1-Jun-1999 12:00 AM

Ca    Wollastonite   1-Jun-1999 12:00 AM

Fe    Fe   1-Jun-1999 12:00 AM

Ni    Ni   1-Jun-1999 12:00 AM

| Element | Weight% | Atomic% | Compd% | Formula |  |
| --- | --- | --- | --- | --- | --- |
| Na K | 0.08 | 0.07 | 0.10 | Na2O |  |
| Mg K | 3.89 | 3.36 | 6.44 | MgO |  |
| Al K | 37.09 | 28.91 | 70.08 | Al2O3 |  |
| Si K | 6.51 | 4.87 | 13.92 | SiO2 |  |
| P K | 0.00 | 0.00 | 0.00 | P2O5 |  |
| S K | 0.64 | 0.42 | 1.59 | SO3 |  |
| Cl K | 0.15 | 0.09 | 0.00 |  |  |
| K K | 0.12 | 0.07 | 0.15 | K2O |  |
| Ca K | -0.11 | -0.06 | -0.15 | CaO |  |
| Fe L | 5.97 | 2.25 | 7.68 | FeO |  |
| Ni L | 0.03 | 0.01 | 0.03 | NiO |  |
| O | 45.64 | 60.00 |  |  |  |
| Totals | 100.00 |  |  |  |  |