## Slide 1: A0026-pFIB02 micro-FTIR analysis at Tohoku U.
2021/09/10
Tohoku University
Kana Amano and Eiichi Kagawa

## Slide 2: Spectra identification
12 | 13 | 14 | 15
08 | 09 | 10 | 11
04 | 05 | 06 | 07
00 | 01 | 02 | 03
12 | 13 | 14 | 15
08 | 09 | 10 | 11
04 | 05 | 06 | 07
00 | 01 | 02 | 03
aperture 160x160 µm2
aperture 100x100 µm2
Colored boxes show the area probed by NanoIR (estimated, not-to-scale)
The number (00 to 15) indicates the ID of the microFTIR spectra (placed in the file name as suffix).
contaminated by carbon glue
Area 27
Flat A

## Slide 3: NanoIR probed area (Area 27)

## Slide 4: pFIBed sample (ID: A0026-pFIB02)
5 mm
pFIBed surface

## Slide 5
12.5 mm
Carbon paste
Sample
(~1mm in size)
Al stage
6~7 mm
3 mm
<1 mm
The pole extends from the center of the disk
From above
From the side
The pFIBed surface is almost parallel to the bottom
※The Al pole is not self-standing.
※The Al pole can be removed from the brown resin holder
Sample preparation
~3 mm

## Slide 6
A0026-pFIB02 (stage tilt: -35°)
Carbon glue contamination

## Slide 7: Analytical summary
・Sample
A0026-pFIB02 (800x600 µm in size, cut and cleaned by pFIB)
A0026 was a mm-sized grain from Room A (Touch Down site 1 on Ryugu).
・micro-FTIR analysis at Tohoku U (Bruker, HYPERION 2000, λ: 2.5-16.5 µm)
Measurement 1
2
Measurement | Aims | Aperture | Point | Scan
1 | Whole surface mapping without contamination of carbon glue | 160x160 µm/pix | 4x4 | 2048
2 | Detailed surface mapping | 100x100 µm/pix | 4x4 | 3072
Carbon glue contamination

## Slide 8: Measurement 1 whole mapping (160x160 µm/pix)
Wavelength (µm)
Reflectance (%)
(!) Each dot in the left figure indicates the center position of the pixel.
Average spectrum of the main area (marked in magenta)
・hydrated minerals (2.7 µm) ・3.1 µm absorption
・aliphatic compounds (3.4 µm) ・carbonates (3.4, 3.95… µm)
・CI-like Si-O band (~10 µm)
Mg-OH
-CH
atmospheric CO2

## Slide 9: Measurement 1 whole mapping (160x160 µm/pix)
Wavelength (µm)
Reflectance (%)
(!) Each dot in the left figure indicates the center position of the pixel.
Each spectrum of the main area (marked in different colors)
・hydrated minerals (2.7 µm)
・3.1 µm absorption
・aliphatic compounds (3.4 µm)
・carbonates (3.4, 3.95… µm)
・CI-like Si-O band (~10 µm)
Wavelength (µm)
Reflectance (%)

## Slide 10: Measurement 2 detailed mapping (100x100 µm/pix)
Wavelength (µm)
Reflectance (%)
(!) Each dot in the left figure indicates the center position of the pixel.
Each spectrum of the main area (marked in different colors)
carbonates?
phyllosilicates

## Slide 11: Measurement 2 detailed mapping (100x100 µm/pix)
Wavelength (µm)
Reflectance (%)
(!) Each dot in the left figure indicates the center position of the pixel.
Each spectrum of the main area (marked in different colors)
・Heterogeneous distribution of carbonates and organic compounds
・Some spectra show 3.1 µm absorption band. What is the origin?
→IR-spectral results can be compared with SEM observations later
2.70:Mg-OH
3.4:-CH
carbonates